## Slide 1: High-pressure Hydrogen Pipeline Systems
The status quo and the new Code of Practice

## Slide 2: It all begins with…
AS(/NZS) 2885…

## Slide 3
AS(/NZS) 2885 series Standards are not intended to prohibit the use of any materials, designs, methods of assembly, procedures or practices (items) that do not conform with specific requirements of the AS(/NZS) 2885 series, or are not mentioned in it, but do give equivalent or better results to those specified.
High Pressure Hydrogen Pipeline Systems

## Slide 4
The Licensee shall ensure the suitability of the item is determined against the fundamental principles of the AS(/NZS) 2885 series, and any additional requirements (including technical, quality, procedural, safety, maintenance) needed to satisfy the fundamental principles shall be developed. Prior to the item being used it shall be approved.
What “fundamental principles” ?
High Pressure Hydrogen Pipeline Systems

## Slide 5
Function
Storage capacity
Energy delivery capacity
Design solution
Diameter, MAOP,
Pressure cycling
Dysfunction
Plastic collapse, Fracture, Fatigue, Impact, Ground-movement, Flotation, Corrosion, Erosion, Internal blockage, etc. etc.
Design solution
Strength, Toughness, Thickness, Cathodic protection, Coating, etc. etc.
Design for function
Design against dysfunction
Design is finding solutions
High Pressure Hydrogen Pipeline Systems

## Slide 6: Design for function
AS 2885:
Doesn’t say much about function…
High Pressure Hydrogen Pipeline Systems
DESIGN CAPACITY
LOAD
(but the new code of practice does)

## Slide 7: Design against dysfunction
AS 2885:
Provides methods to determine design capacity, and
Is a repository of industry ‘best-practice’ methods.
DESIGN CAPACITY
THREAT
BUT not all dysfunction can be “solved”.
Events that exceed the design capacity will always be possible.
High Pressure Hydrogen Pipeline Systems

## Slide 8: Fundamental principles…
“Residual” risk

## Slide 9: Solving problems managing “residual” risk
Minimal risk (ALARP)
Acceptable risk (individual, societal, environmental)
High Pressure Hydrogen Pipeline Systems

## Slide 10: Incident sequence
Cause
Failure Mode
Effect
Consequence
Fault sequence
Design controls
Mitigation controls
Threat controls
Responsive actions
Material properties
Gas properties
H2-affected inputs
High Pressure Hydrogen Pipeline Systems

## Slide 11: Hydrogen service is different to natural gas
Lower toughness
(e.g. to ~55 MPa(m)0.5)
Lower energy density
(1/3 x nat. gas)
Material properties
Gas properties
Higher volumetric flow
(3x nat. gas)
Lower ignition energy
(more auto-ignition)
Higher fatigue rate
(e.g. 1/10x fatigue life)
+ Other adverse effects on other materials
Lower ductility
(though generally post-necking)
Higher flame-speed
(more explosion harm)
High Pressure Hydrogen Pipeline Systems

## Slide 12: Changes to gas properties…
Design for function
When a leak occurs…

## Slide 13: Design for function
At the same pressure…
Energy storage capacity… approx. 1/3rd of NG for same volume/pressure
Energy flow capacity… approx. same as NG, though requires higher velocity
(But a design may not be permitted to operate at the same pressure)
High Pressure Hydrogen Pipeline Systems
NOTE:
For blended pipelines, the worst energy flow rate is not 100% NG, nor 100% H2.
The lowest energy flowrate would typically occur at about 80% H2 (20% NG).

## Slide 14: When a leak occurs…
Initially…
Dispersed cloud size… larger,
Ignition becomes much more likely
Energy release rate… approximately the same as NG (1/3x and 3x cancel each other out)
High Pressure Hydrogen Pipeline Systems

## Slide 15: When a leak occurs…
Higher flame-speed also means…
Greater potential harm from over-pressure waves
Depends on ‘delayed ignition’ potential, which seems unlikely
Q: What is detonation?
A: A speed-of-sound explosion that occurs if the over-pressure wave ahead of the flame-front becomes hot enough for auto-ignition.
High Pressure Hydrogen Pipeline Systems

## Slide 16: Changes to material properties…
Toughness
Fatigue crack growth

## Slide 17: Importance of material property changes - toughness
What it is:
When a pipe fails, the difference between rupture (“burst”) and leak is affected by toughness.
‘Hydrogen embrittlement’ may mean rupture occurs when it previously would not have.
Hence, toughness affects:
Safety management – the “critical defect length” reduces!
“No rupture” determinations
Fitness for service assessments of sharp defects (e.g. SCC)
Hydrotest effectiveness. Is it still a proof test?
High Pressure Hydrogen Pipeline Systems

## Slide 18: Importance of material property changes - toughness
Measuring the toughness… what a ride!
Historical Charpy testing – not suitable, cannot be done in hydrogen
ASME B31.12 – endorsed AS1681, also not suitable
    Loaded before charging, hence non-conservative
    Designed for sub-critical growth, which doesn’t generally occur in H2-gas
    55 MPa(m)0.5 is a low bar, equivalent to about 1.2J Charpy!
ASTM1820 – tensile toughness test
    Provides J-R curve
    But, single-variable representation is most commonly reported (KIC, JIC, δ)
    And single-variable removes data, and underestimates total resistance to fracture
So… we must use complex ductile tearing analysis, or conservative assumptions!
High Pressure Hydrogen Pipeline Systems

## Slide 19: Importance of material property changes - toughness
DAMAGE
PRESSURE
FLUID
MATERIAL
Size & sharpness
Hoop stress
Toughness & Strength
Decompression
Failure mode factors
How bad is it?
Toughness is not the only factor! Reduced stress design.
Current evidence: hydrogen is an equalizer.
Effect reduces at low partial pressures, though difficult to account for, with…
No predictive models .
High Pressure Hydrogen Pipeline Systems

## Slide 20: Importance of material property changes – fatigue growth
What is it?
The growth rate of existing cracks is accelerated in the presence of hydrogen!
In this case, good predictive models exist  e.g. SANDIA (ASME CC2938) and NIST (ASME B31.12).
High Pressure Hydrogen Pipeline Systems

## Slide 21: Importance of material property changes – fatigue growth
Fatigue life affects:
Most concerning/pertinent for gas storage applications.
Complex analysis is required:
  Initial defect size?
  Final defect condition?
  Use outside the models’ calibrated parameters.
There are mitigating factors that can’t be accommodated in analysis (e.g. crack rounding from hydrotest, internal vs external, etc.)
Q: Does concentration matter?
A: Not directly. For material effects, the partial pressure matters.
AND the effects of H2 become apparent even at low partial pressures.
High Pressure Hydrogen Pipeline Systems

## Slide 22: So, about the code of practice…

## Slide 23: Integrating into the “fundamental principles”
Cause
Failure Mode
Effect
Consequence
Fault sequence
Design controls
Mitigation controls
Threat controls
Responsive actions
Material properties
Gas properties
H2-affected inputs
High Pressure Hydrogen Pipeline Systems

## Slide 24: Example: excavator strike
Excavator hit
Pipe burst
Ignited leak
1 burn injury
Decreased toughness (HE)
Increased ignition frequency
Wall thickness and toughness
Automatic line-break valves
Marker signs and tape
Fault sequence
Responsive actions
H2-affected inputs
High Pressure Hydrogen Pipeline Systems

## Slide 25: The Code of Practice!
Developed by FFCRC, with GPA leading the project execution
Addresses both function and dysfunction
Addresses a lot more than this presentation has!
Provides methods for analysis, broad assumptions, guidelines for material testing, and commentary
Matches/complements the performance-based standardization of AS/NZS 2885
But is NOT a standard
Hasn’t yet been published…
High Pressure Hydrogen Pipeline Systems